CERTIFICATE OF ANALYSIS

SECTION 1. PRODUCT AND COMPANY IDENTIFICATION

Product name: Cosmetic Grade Glitter

Product code: FCH884

Production date: Feb. 11, 2020~ Feb.18, 2020

Expiry date: Feb. 18, 2023

Supplier: Zhongshan Zhongtai Pigment Co., Ltd.

SECTION 2. INFORMATION ON SPECIFICATION

| Product Code | Color | Thickness | Solvent- resistance | Heat Resistance | Light/UV Resistance | Shape | size | FD&C Colorant | D&C Colorant | Pigment | PH Value | Surface Degradability |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| FCH884 | Chameleonic | 36μm | ✘ | 120~150℃ | 3.5 | Hexagon | 0.08~3mm | ✔ | - | - | 7.0~7.5 | ✔ |

SECTION 3. INFORMATION ON INGREDIENTS

| Key Ingredient | CAS NO. | EC NO. | Target% |
| --- | --- | --- | --- |
| Polybutylene Terephthalate | 26062-94-2 | 607-857-5 | 93.8 |
| Acrylates copolymer | 25133-97-5 | 607-559-5 | 2.8 |
| Carbon Black (C.I. 77266) | 1333-86-4 | 215-609-9 | 3.4 |

SECTION 4. TEST REPORT ON HEAVY METALS