CERTIFICATE OF ANALYSIS

SECTION 1. PRODUCT AND COMPANY IDENTIFICATION

Product name: Cosmetic Grade Holographic Black Glitter

Product code: FCHL1000

Production date: Feb. 04, 2020 ~ Feb.22, 2020

Expiry date: Feb. 21, 2023

Supplier: Zhongshan Zhongtai Pigment Co., Ltd.

SECTION 2. INFORMATION ON SPECIFICATION

| Product Code | Color | Thickness | Solvent- resistance | Heat Resistance | Light/UV Resistance | Shape | size | FD&C Colorant | D&C Colorant | Pigment | PH Value | Surface Degradability |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| FCHL1000 | Holographic Black | 25μm |  | 170~190℃ | 8 | Hexagon | 0.08mm-3.0mm | - |  | - | 7.5 |  |

SECTION 3. INFORMATION ON INGREDIENTS

| Key Ingredient | CAS NO. | EC NO. | Target% |
| --- | --- | --- | --- |
| Polyethylene terephthalate | 25038-59-9 | 607-507-1 | 97.86 |
| Acrylates copolymer | 25133-97-5 | 607-559-5 | 1.8 |
| Aluminum | 7429-90-5 | 231-072-3 | 0.01 |
| Carbon Black (C.I. 77266) | 1333-86-4 | 215-609-9 | 0.33 |

SECTION 4. TEST REPORT ON HEAVY METALS