CERTIFICATE OF ANALYSIS

SECTION 1. PRODUCT AND COMPANY IDENTIFICATION

Product name: Cosmetic Grade Glitter

Product code: FCHL901	Batch Number:20200211-B02 Production date: Feb. 11, 2020 ~ Feb.18, 2020

Expiry date: Feb. 18, 2023

Supplier: Zhongshan Zhongtai Pigment Co., Ltd.

SECTION 2. INFORMATION ON SPECIFICATION

| Product Code | Color | Thickness | Solvent- resistance | Heat Resistance | Light/UV Resistance | Shape | size | FD&C Colorant | D&C Colorant | Pigment | PH Value | Surface Degradability |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| FCHL901 | Holographic peach red | 25/50μm | ✔ | 170~190℃ | 7 | Hexagon/Special Shapes | 0.08~3mm | - | - | ✔ | 7.5 | ✘ |

SECTION 3. INFORMATION ON INGREDIENTS

| Key Ingredient | CAS NO. | EC NO. | Target% |
| --- | --- | --- | --- |
| Polyethylene terephthalate | 25038-59-9 | 607-507-1 | 97.87 |
| Acrylates copolymer | 25133-97-5 | 607-599-5 | 1.8 |
| Aluminum | 7429-90-5 | 231-072-3 | 0.01 |
| FD&C Red 40 (CI.16035) | 25956-17-6 | 247-368-0 | 0.06 |
| D&C Red 27 (C.I.45410:2) | 15876-58-1 | 240-012-5 | 0.26 |

SECTION 4. TEST REPORT ON HEAVY METALS