CERTIFICATE OF ANALYSIS

SECTION 1. PRODUCT AND COMPANY IDENTIFICATION

Product name: Cosmetic Grade Holographic Blue Purple Glitter Product code: FCHL800

Production date: Feb. 04, 2020 ~ Feb.22, 2020

Expiry date: Feb. 21, 2023

Supplier: Zhongshan Zhongtai Pigment Co., Ltd.

SECTION 2. INFORMATION ON SPECIFICATION

| Product Code | Color | Thickness | Solvent- resistance | Heat Resistance | Light/UV Resistance | Shape | size | FD&C Colorant | D&C Colorant | Pigment | PH Value | Surface Degradability |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| FCHL800 | Holographic Blue Purple | 25μm |  | 160~170℃ | 3 | Hexagon | 0.08mm-3.0mm |  | - | - | 7.8 |  |

SECTION 3. INFORMATION ON INGREDIENTS

| Key Ingredient | CAS NO. | EC NO. | Target% |
| --- | --- | --- | --- |
| Polyethylene terephthalate | 25038-59-9 | 607-507-1 | 97.22 |
| Acrylates copolymer | 25133-97-5 | 607-559-5 | 1.8 |
| Aluminum | 7429-90-5 | 231-072-3 | 0.01 |
| FD&C Blue 1（C.I.42090） | 3844-45-9 | 223-339-8 | 0.11 |
| D&C Red 27 (C.I.45410:2) | 15876-58-1 | 240-012-5 | 0.66 |
| FD&C Red 40 (CI.16035) | 25956-17-6 | 247-368-0 | 0.2 |

SECTION 4. TEST REPORT ON HEAVY METALS