CERTIFICATE OF ANALYSIS

SECTION 1. PRODUCT AND COMPANY IDENTIFICATION

Product name: Cosmetic Grade Glitter

Product code: FCH34	batch number:20200206-A03 Production date: Feb. 11, 2020 ~ Feb.18, 2020

Expiry date: Feb. 18, 2023

Supplier: Zhongshan Zhongtai Pigment Co., Ltd.

SECTION 2. INFORMATION ON SPECIFICATION

| Product Code | Color | Thickness | Solvent- resistance | Heat Resistance | Light/UV Resistance | Shape | size | FD&C Colorant | D&C Colorant | Pigment | PH Value | Surface Degradability |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| FCH34 | Colorful Orange | 25/50μm | ✔ | 170~190℃ | 5 | Hexagon /Special Shapes | 0.08~3mm | - | - | ✔ | 7.5~8 | ✘ |

SECTION 3. INFORMATION ON INGREDIENTS

| Key Ingredient | CAS NO. | EC NO. | Target% |
| --- | --- | --- | --- |
| Polybutylene Terephthalate | 26062-94-2 | 607-857-5 | 98.34 |
| Acrylates copolymer | 25133-97-5 | 607-559-5 | 1.3 |
| Aluminum | 7429-90-5 | 231-072-3 | 0.01 |
| FD&C Yellow 5 (CI.19140) | 1934-21-0 | 217-699-5 | 0.13 |
| FD&C Red 40（CI.16035） | 25956-17-6 | 247-368-0 | 0.22 |

SECTION 4. TEST REPORT ON HEAVY METALS