CERTIFICATE OF ANALYSIS

SECTION 1. PRODUCT AND COMPANY IDENTIFICATION

Product name: Cosmetic Grade Iridescent Glitter Product code: FCH22

Production date: Feb. 04, 2020 ~ Feb.22, 2020

Expiry date: Feb. 21, 2023

Supplier: Zhongshan Zhongtai Pigment Co., Ltd.

SECTION 2. INFORMATION ON SPECIFICATION

| Product Code | Color | Thickness | Solvent- resistance | Heat Resistance | Light/UV Resistance | Shape | size | FD&C Colorant | D&C Colorant | Pigment | PH Value | Surface Degradability |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| FCH22 | Iridescent | 36μm |  | 120~150℃ | 8 | Hexagon | 0.08mm-3.0mm | - | - | - | 7.8 |  |

SECTION 3. INFORMATION ON INGREDIENTS

| Key Ingredient | CAS NO. | EC NO. | Target% |
| --- | --- | --- | --- |
| Polybutylene Terephthalate | 26062-94-2 | 607-857-5 | 99.3 |
| Acrylates Copolymer | 25133-97-5 | 607-559-5 | 0.7 |

SECTION 4. TEST REPORT ON HEAVY METALS